Nanofiltration Performance of Lead Solution: Effects of concentration,

solution pH and ionic strength

Wuthikorn Saikaewa*, Supatpong Mattarajb, and Ratana Jiraratananonc

a*Faculty of Engineering, Ubon Ratchathani University, Warinchumrab,

Ubon Ratchathani, Thailand; Email: k.saikaew@thaimail.com

bDepartment of Chemical Engineering, Faculty of Engineering, Ubon Ratchathani University

Ubon Ratchathani, Thailand.

cDepartment of Chemical Engineering, King Mongkut’s University of Technology Thonburi, Bangkok, Thailand.

*Corresponding author: k.saikaew@thaimail.com

Abstract

# The effects of solution chemistry (i.e. concentration, solution pH and ionic strength) on nanofiltration system were investigated using a dead-end test cell at room temperature. An aromatic polyamide NF-90 membrane was chosen to determine the impacts of solution chemistry on nanofiltration fouling of lead solution (i.e. PbCl2, Pb(NO3)2). The experimental results revealed that solution flux decline was dependent on concentration, solution pH and ionic strength. The higher solution concentrations showed greater flux decline and rejection. Flux decline conducted with lead solution decreased for solution pH. At high pH, flux solutions showed higher flux decline than those of low solution pH, while the ions rejection presented higher rejection. Increased ionic strength had a greater increase in flux decline. Lead ion rejection was found to be decreased with decreasing solution pH and increasing ionic strength. Flux and rejection decreased further in the higher ionic strength, which reduced negatively charged repulsion on the membrane surface, and thus decreased rejection. Furthermore, the comparisons on flux decline for co-ions were also investigated during filtration experiments.

# Keywords: Flux decline, Fouling, Lead, Nanofiltration, Rejection

1. Introduction

The occurrences of metal ions in the aquatic environment have been concern because of their toxicity, while accumulation may pose various hazards for human health and environment. At the present, the most frequency practiced treatment technology for the removal of metal ions from aqueous solution is chemical precipitation, which only relocated metal ions from aqueous phase, leave further sludge problems to be solved. Therefore, the removal of metal ions from many industrial wastewaters has stimulated vigorous research activities in the development of appropriated treatment technologies. Membrane separation technologies have been determined to be a feasible option for removal of heavy metal from aqueous solution because of its relative ease of construction and control, and the feasible recovery of valuable metals. These technologies have been widely used in the field of water treatment due to stringent water quality regulations [1]. They are efficient technologies to remove feed source water in terms of natural organic matter (NOM) [1-5], inorganic scalants [6-8], salt solution [9-11] and heavy metals [12-16]. Nanofiltration (NF), one of membrane technologies, is a relatively new membrane process, which is considered to be intermediate between ultrafiltration (UF) and reverse osmosis (RO) in terms of operating conditions. NF membrane processes operate at pressures between 50 and 150 psi much lower than RO (200 to 1000 psi), but higher than UF (10 to 70 psi). At the present time, NF is increasingly applied in the field of water treatment. However, membrane fouling caused by organic and inorganic substances can be a major factor for limiting more widespread use of membrane technologies, reducing long-term filtration, and increasing costs for membrane operation through higher labor, cleaning and replacement. Inorganic fouling (i.e. negative and positive ions) can be a significant factor that enhances permeate flux decline during filtration. This may cause an increased concentration polarization that exceeds solubility limit, resulting precipitation (i.e. Ca2+, Mg2+, CO32−, SO42−, and PO43−). This has been recently investigated by Jarusutthirak et al. [8]. Molinari et al. [13] investigated the interactions between membranes (RO and NF) and inorganic pollutants (i.e.SiO2, NO3−, Mn++, and humic acid). They showed that membrane fouling was caused by the interactions between the membranes and other ions. Other factors, which can cause membrane fouling, are solution pH, ionic strength, concentration, solution composition, and operating conditions. Lead is a hazardous waste and is highly toxic to humans, plants and animals. It causes plant and animal death as well as anemia, brain damage, mental deficiency, anorexia, vomiting and malaise in humans [17-18]. Lead is a substitute for calcium in bony tissues and accumulates there. The presence of lead in drinking water is known to cause various types of serious health problems leading to death in extreme cases. [19]. The allowed concentration in drinking water of lead is about 0.1 mg/L [20].

The objective of this work was to investigate the effects of solution chemistry during nanofiltration of lead solution.  The effects of solution chemistry (i.e. concentration, solution pH and ionic strength) were determined on nanofiltration fouling. The discussion of this study was further adapted to improve membrane filtration for long-term operation.

2. Experimental

# 2.1 Nanofiltration Characteristics

An aromatic polyamide thin-film composite NF-90 membrane, produced by Dow-FilmTec., was chosen to determine the effect of solution chemistry on nanofiltration performance. According to the manufacturer, the maximum operating pressure is 600 psi (or 4,137.6 kPa), maximum feed flow rate is 16 gpm (3.6 m3/hr), maximum operating temperature 113°F (45°C) and the operating pH is ranged from 1 to 12.

# 2.2 Analytical Method

# Lead ion concentration was measured by using atomic absorption (AA) spectrometry (AAnalyst 200 Version 2, Perkin Elmer Corp.). Measurements of solution pH, conductivity and temperature were made using pH meter (Inolab pH level 1 Wissenschaftlich- Technische Werkstatten (WTW) Gmbh & Co. (Weilheim,Germany)), and conductivity meter (Inolab cond level 2 Wissenschaftlich-Technische Werkstatten (WTW) Gmbh & Co. (Weilheim,Germany)), respectively. Ionic strengths were calculated using a correlation between conductivity and ionic strength of  NaCl standard, I.S.[M]=0.5∑CiZi2 (Ci is the ion concentration and Zi is the number of ions).

# 2.3 Flux decline experiments

The experiments were carried out with three liters of solution containing lead solution (PbCl2 and Pb(NO3)2) in varied concentration of 10, 20, 30 and 50 mg/L, while varying solution pH from 4 to 6 and ionic strengths (0.01, 0.05 M as NaCl). Flux decline experiments were tested by using a 400-ml dead-end membrane filtration apparatus (Amicon 8400, USA) with magnetic stirrer (LABINCO, LD-12) and the magnetic spin bar was fitted into the cell including agitation speed. A membrane sheet can be fitted to the cell. The membrane active area is about 41.38 cm2. The operating pressure was employed via high-pressure regulator of nitrogen cylinder. The permeate flux was kept in a beaker on the electrical balances (Mettler Toledo Monobloc PB-3002-S, USA).

2.4 Filtration Experiments

Membrane sheets were rinsed with cleaned DI water, citric acid solution of pH 4, and followed with sodium hydroxide solution of pH 10 for 30-min each. Cleaned water flux was determined with a function of transmembrane pressure. Cleaned DI water was subsequently tested for 30-min membrane compaction with velocity rate of 300 rpm. Cleaned water flux was subsequently determined with increased operating pressures before lead solution was used with the system. Feed lead solutions were prepared for each tested condition. After filtration was terminated, two steps of cleaning, i.e. hydrodynamic cleaning followed by chemical cleaning, were performed. For hydrodynamic cleaning, the membrane sheet was cleaned with DI water, then followed with chemical cleaning, acidic solution (using citric acid) with pH of 4 for 30-min each. After each cleaning, water fluxes at different operating pressures were measured to determine water flux recovery.

# 2.5 Analysis of Results

The parameters taken into account were:

- The volumetric flux Jv (L/m2/h or LMH) was determined by measuring the volume of permeate collected in a given time interval divided with membrane area by the relation:

(1)

Where, Q and A represents flow rate of permeate and the membrane area, respectively.

- The observed rejection was calculated by the following relation:

(2)

Where Cp and Ci are the solution concentrations in the permeate and in the initial feed solution, respectively.

3. Results and Discussions

3.1Effect of solution concentration on flux decline and rejection

In order to determine the effect of metal concentration on flux decline and rejection, lead ion concentrations were varied for 10, 20, 30 and 50 mg/L at pH 6 and ionic strength of 0.01 M NaCl. As shown in Fig.1 and 2, it can be concluded that lead ion rejection and solution flux decline increased with increasing solution concentrations. The higher solution concentrations for PbCl2 solution had greater ion rejection, about 94%-98 %, while low solution concentration exhibited lower rejection about 85%-87%. For Pb(NO3)2 solutions having 50-mg/L concentration had the ion rejection about 98-99%, while those of the lower concentrations were 88-95%.

(a)

(b)

Fig.1 Effect of solution concentration on flux decline; (a) PbCl2 and (b) Pb(NO3)2

(a)

(b)

Fig.2 Effect of concentration on rejection; (a) PbCl2 and (b) Pb(NO3)2

3.2 Effects of solution pH on flux

# The effects of  solution pH on flux decline of PbCl2 and Pb(NO3)2 solution were carried out at pH 4,5 and 6 with keeping constant ionic strength 0.01 M as NaCl at 60-psi operating pressure. Lead concentration was about 20 mg/L. Fig. 3 showed relative flux with function of operating period for PbCl2 and Pb(NO3)2 solution. It can be seen that the rate and extent of flux decline increased with increasing solution pH. For the solution of PbCl2 and Pb(NO3)2 solution at lower pH, flux solutions showed higher flux decline than those of low solution pH.  At low pH, it suggested an increased fixed charge of H(, decreasing electrical double layer thickness within membrane or both, thus decreased the concentration at the membrane surface. At high pH, the membrane surface and pores become both more negatively charged due to the presence of anion (inorganic). In addition, the osmotic pressure near the membrane surface increase with high salt rejections, thus decreasing the driving pressure. These mechanisms lead to a decrease in permeate flux and an increase in salt rejection with pH.

# (a)

(b)

Fig.3 Effect of solution pH on Flux decline; (a) PbCl2 and (b) Pb(NO3)2

# 3.3 Effects of solution pH on rejection

# The effects of the solution pH on rejection of PbCl2 and Pb(NO3)2 solution was carried out with different solution  pH from 4 to 6.  Solution was maintained constant with Ionic strength of 0.01 M NaCl, 60 psi operating pressure and solution concentration of 20 mg/L during filtration. The obtained results were presented in Fig.4.  Lead ion rejection was found to be decreased with decreasing solution pH level. It was possibly due to higher solution pH, membrane surface take more negative charges, thus attracting greater lead ion. Consequently, solution pH of 5-6 for PbCl2 had greater ion rejection about 96%-98 %, while low solution pH exhibited lower rejection about 88%-91%. For Pb(NO3)2 solution, the ion rejection percentages of higher solution pH (5-6) and lower solution pH were 91-94 % and 76-81 %, respectively.

(a)

(b)

Fig.4 Effect of solution pH of on rejection; (a) PbCl2 and (b) Pb(NO3)2

# 3.4 Effects of ionic strength on flux

Fig.5 presents the effect of ionic strength on flux that was carried out at pH 6 with different ionic strengths of 0.01 and 0.05 M as NaCl. It was observed that the extent and rate of solution flux decline increased with increasing ionic strength.  In the study, increases in ion concentration can reduce the permeability of charged membranes [21-22], thus reduced permeate flux. The results showed the similar trend for both of 20 mg/L PbCl2 and Pb(NO3)2 solution.

(a)

(b)

Fig.5 Effect of ionic strength on flux decline; (a) PbCl2 and (b) Pb(NO3)2

# 3.5 Effect of ionic strength on lead ion rejection

# The effect of salt solution on lead ion rejection were carried out with ionic strengths of 0.01 and 0.05 M as NaCl and the concentration of 20 mg/L, as shown in Fig.6.  Solution pH of 6 for PbCl2 and Pb(NO3)2 solution was kept constant during filtration. It was found that lead rejection at ionic strength of 0.05 M showed lower than those at ionic strength of 0.01 M. This was possibly due to increasing salt concentration, reducing membrane permeability, thus allowing lead ion passage through the membrane surface.

# (a)

# (b)

Fig. 6  Effect of ionic strength on lead ion rejection; (a) PbCl2 and (b) Pb(NO3)2

3.6 Effect of co-ion on solution flux decline

The effect of the co-ion on lead solution flux decline was carried out with two types of Pb2+ (PbCl2 and Pb(NO3)2) solution at the concentration of 20 mg/L. The experiments were performed at pH 6, ionic strength of 0.01 M NaCl and 60 psi operating pressure during filtration. From the experiment, it can be seen that Pb(NO3)2 solution had a slight lower on flux decline than PbCl2 solution. PbCl2 solution showed higher rejection than Pb(NO3)2 solution. Since the NF membrane is more negatively charged, the monovalent anion of Cl- is more excluded than NO3- resulting in greater rejection. Furthermore, the ion rejection is mainly dependent on its hydration energy in the solution and it was more retained if it has higher hydration energy, in accordance with the mechanism of solution-diffusion [23-24]. The hydration energy of Cl- and NO3- are 372 KJ/mol and 328 KJ/mol respectively [23]. However, the higher rejection of chlorides can not be described by the hydration energy owning to the fact that these anions had close hydration energy. It can be explained by the formation of the complexes solution, which involves an electrostatic repulsion with charge membrane and thereafter a strong rejection of the ions.

4. Conclusion

Lead ions rejection and flux decline from aqueous solution by nanofiltration was strongly influenced by concentrations, solution pH and ionic strength. Flux decline conducted both in PbCl2 and Pb(NO3)2 solution decreased for solution pH and concentrations. At higher solution pH, flux solutions showed higher flux decline than those of low solution pH, while lead rejection exhibited higher rejection. Increased ionic strength had a greater increase in flux decline. Lead ion rejection was found to be decreased with decreasing concentrations, solution pH and increasing ionic strength.

5. Acknowledgement

This work was financially supported by Commission on Higher Education, Ministry of Education, Thailand and Professor Dr. Ratana Jiraratananon as the head of Senior Membrane Technology Project. The authors are also grateful to the faculties for their assistance during experiments at the chemical engineering laboratory, Ubon Ratchathani University.

6. References

[1] Hong S., and Elimelech M., Chemical and Physical Aspects of Natural Organic Matter (NOM) Fouling of Nanofiltration Membranes, J. Membrane Science, Vol.132, pp.159-181, 1997.

[2] Alborzfar M., Jonsson G., and Gron C., Removal of Natural Organic Matter from Two Types of Humic Ground Waters by  Nanofiltration, Water Research, Vol. 32, No.10, pp.2983-2994. 1998.

[3] Cho J., Amy G., and Pellegrino J., Membrane Filtration of Natural Organic Matter: Initial Comparison of Rejection and Flux Decline Characteristics with Ultrafiltration and Nanofiltration Membranes, Water Research, Vol.33, No. 11, pp. 2517-2526, 1999.

[4] Schafer A.I., Fane A. G., and Waite T. D., Fouling Effects on Rejection in the Membrane Filtration of Natural Waters, Desalination, Vol.131, pp. 215-224, 2000.

[5] Kilduff J. E., Mattaraj S., and Belfort G.,   Flux Decline during Nanofiltration of Naturally-Occurring Dissolved Organic Matter: Effects of Osmotic Pressure, Membrane Permeability, and Cake Formation, J. Membrane Science, Vol. 239, No.1, pp.39-53, 2004.

[6] Lisdonk C.A.C., van Paassen J.A.M., Schippers J.C., Monitoring Scaling in Nanofiltration and Reverse Osmosis Membrane Systems, Desalination, Vol.132, pp.101-108, 2000.

[7] Lin C.J., Shirazi S., Rao P., Agarwal S.,  Effects of Operational Parameters on Cake Formation of CaSO4 in Nanofiltration,  Water Research, Vol.40, pp.806-816, 2006.

[8] Jarusutthirak C., Mattaraj S., and Jiraratananon R., Influence of Inorganic Scalants and Natural Organic Matter on Nanofiltration Membrane Fouling, J. Membrane Science, Vol. 287, pp.138-145, 2007.

[9] Childress A. E., and Elimelech M., Effect of  Solution Chemistry on the Surface Charge Of  Polymeric Reverse Osmosis and Nanofiltration Membrane, J. Membrane Science, Vol.119, pp.253-268, 2007.

[10] Anne C. O., Trebouet D., Jaouen P., and Quemeneur F., Nanofiltration of Seawater: Fractionation of Mono-and Multi-valent Cations, Desalination, Vol. 140, pp.67-77, 2001.

[11] Labbez C., Fievet P., Szymczyk A., Vidonne A. , Foissy A., and Pagetti J., Retention of  Mineral Salts by a Polyamide Nanofiltration Membrane, Separation and Purification Technology, Vol.30, pp.47-55, 2003.

[12] Mehiguene K., Garba Y., Taha S., Gondrexon N., and Dorange G., Influence of Operating Conditions on the Retention of  Copper and Cadmium in Aqueous Solutions by Nanofiltration: Experimental Results and Modelling, Separation and Purification Technology, Vol.15, pp.181-187, 1999.

[13] Molinari R., Argurio P., and Romeo L., Studies on Interactions between Membranes (RO and NF) and Pollutants (SiO2, NO3−, Mn++, and humic acid) in Water, Desalination, Vol.138, pp.271-281.2001.

[14] Ku Y., Chen S.W., and Wang W.Y., Effect of Solution Composition on the Removal of Copper Ions by Nanofiltration, Separation and Purification Technology, Vol.43, pp.135-142, 2005.

[15] Ipek U., Removal of Ni(II) and Zn(II) from an Aqueous Solution by Reverse Osmosis,   Desalination, Vol.174, pp.161-169, 2005.

[16] Turek M., Dydo P., Trojanowska J., and Campen A., Adsorption/Co- Precipitation-Reverse Osmosis System for Boron Romoval, Desalination, Vol.205, pp.192-199, 2007.

[17] Gaballah, I., Kilbertus, G., Recovery of heavy metal ions through decontamination of synthetic solutions and industrial effluents using modified barks, J. Geochem. Explor., Vol.63, pp.241-286, 1998.

[18] Low, K.S., Lee, C.K., Liew, S.C., Sorption of cadmium and lead from aqueous solutions by spent grain, Process Biochem, Vol.36, pp. 59-64, 2000.

[19] Volesky, B., Removal of lead from aqueous solution by Penicillium biomass, Biotechnol. Bioeng., Vol.42, pp.785-787, 1993.

[20] Ministry of Public Health Notification, The quality of bottled drinking water in Thailand, no. 61, 1981.

[21] Yaroshchuk A., and Staude E., Charged membranes for low pressure reverse osmosis properties and applications, Desalination, Vol.86, pp. 115-134, 1992.

[22] Eriksson P., Water and salt transport through two types polyamide composite membrane, J. Membr. Sci., Vol.36, pp. 297-313, 1988.

[23] A. Darbi, T. Viraraghavan, T.C. Jin, L. Braul and D. Corkal, Sulfate removal from water, Water Qual. Res. J., Vol. 38, No.1, pp.169-182, 2003.

[24] I. Novak, L. Sipos and B. Kunst, Removal of sulfates and other inorganics from potable water by nanofiltration membranes of characterized porosity, Separ. Purif. Technol., Vol.37, pp.177-185, 2004.